## Slide 1
Nucleation Benchmark Problem
Wenkun Wua,d, David Taboadab, Jonathan Guyerc, Olle Heinonend,e, James Warrenc, Peter Voorheesa,f, Daniel Wheelerc, László Gránásyg and Tamás Pusztaig
a Center for Hierarchical Materials Design, Northwestern University, 2205 Tech Drive, Suite, 1160, Evanston, IL, 60208, USA
b Department of Materials Science and Engineering, University of Michigan, 2300 Hayward St., Ann Arbor, MI 48106, USA
c Materials Measurement Laboratory, National Institute of Science and Technology, 100 Bureau Drive, MS8300, Gaithersburg, MD 20900-8300
d Materials Science Division, Argonne National Laboratory, 9700 South Cass Avenue, Lemont, IL, 60439, USA
e Northwestern-Argonne Institute of Science and Engineering, 2205 Tech Drive, Suite 1160, Evanston, IL, 60208, USA
f Department of Material Science and Engineering, Northwestern University, 2220 Campus Drive, Evanston, IL, 60208, USA
g Research Institute for Solid State Physics and Optics, P.O. Box 49, H-1525 Budapest, Hungary

## Slide 2: Problem Setup
5
Free energy:
Time evolution of ɸ given by the Allen-Cahn equation:
Initial condition:
Unit length – width of the interface:
Interfacial energy:
driving force for solidification

## Slide 3: 1. Explicit Nucleation: Single Seed
24
System size: 100 x 100
Run three simulations with different initial nucleus radius
Follow the time evolution of the system for t = 100 units, and plot the solid fraction X and the total free energy F as function of time
No-flux boundary condition
The result for may not be the same due to numerical issues with convergence. Compare your result with the gold standard solution for
t=0

## Slide 4
7
Finite Difference
Free Energies
PRISMS-PF
F
t
MOOSE
FiPy

## Slide 5
8
Solid Fraction
nucleus shrinks
MOOSE
FiPy
Finite Difference
nucleus grows
X
t
PRISMS-PF

## Slide 6: Convergence Test for Single Seed Nucleation
29
Gold standard solution
(finest part Δx=0.1)

## Slide 7: 2. Explicit Nucleation: Multiple Seeds at t=0
System size:
Run the simulation until t = 300. By this time, the whole domain should be transformed to solid
Plot the time evolution of the total free energy, total number of particles, volume fraction, and make the Avrami plot. The slope of the Avrami plot should be close to n=2
Generate random positions with uniform distribution for 25 supercritical seeds with at t=0
25
No-flux boundary condition
500 x 500
t=80

## Slide 8: Total Energy, Volume Fraction, Particle Count and Avrami Plot for Five Runs with Different RNG Seeds
33
Initial nuclei only: n=d
Notes: Average slope = 2.27

## Slide 9: 3. Explicit Nucleation: Multiple Seeds at Random Times
26
System size: 1000 x 1000
Generate 100 random nucleation times in the range t=0~600 for adding the 100 supercritical seeds with to the simulation domain at random positions
Run the simulation until t = 600. By this time, the whole domain should be transformed to solid
Plot the time evolution of the total free energy, the total number of particles, the volume fraction, and make the Avrami plot. The slope of the Avrami plot should be close to n=3
No-flux boundary condition
t=100

## Slide 10: Total Energy, Volume Fraction, Particle Count and Avrami Plot for Five Runs with Different RNG Seeds
33
Constant nucleation rate: n=d+1
Notes: Average slope = 3.00

## Slide 11: 4. Athermal Nucleation
27
System size: 40 x 20
Run the simulation until t=6500, and plot the solid fraction X. Show the snapshot of the phase-field at t=6500
Dirichlet boundary conditions on the bottom: along the middle part of length 20 of the boundary and outside. No-flux boundary conditions for the other three sides
Run four simulations with different driving force:
The result for may not be the same due to numerical issues with convergence. Compare your result with the gold standard solution for

## Slide 12
21
Solid Fraction
Finite Difference
PRISMS-PF
X
t
MOOSE
FiPy
Adaptive meshing:
at the interface
Adaptive time stepper:
from the beginning

## Slide 13: Convergence Test for Athermal Nucleation
30
Gold standard solution
(finest part Δx=0.025)